Temperature dependent structural phase transformation from nano to microstructures: A real time TEM study

Umananda M. Bhatta1**, J. Ghatak1, A. Rath1, J. K. Dash1, P. Santhana Raman2, P.V.Satyam1*

1Institute of Physics, Bhubaneswar

2 Material Science Division, Indira Gandhi Centre for Atomic Research, Kalpakkam

*Email: satyam@iopb.res.in

**Presenting Author

#### Abstract

We report temperature dependent real-time TEM studies on the growth of self-assembled  AuSi microstructures on Si(110) surfaces. Thin Au films ((2 nm) were deposited under the following surface conditions: a) native SiO2/Si(110) and b) MBE – Si(110). Planar TEM micrographs of as deposited systems show isolated nano structures in both the cases. Real time in-situ TEM measurements were carried out at various temperatures (RT to 1000˚C). At higher temperatures these nanostructures were found to grow into nano/micron size rod-like structures, all aligned in one direction. Selected area diffraction (SAD) of these structures reveal the formation of gold silicide (AuxSiy) with different stoichiometry in MBE and the other system.